## Slide 1
Background Fig. 1 Cycle diagram of ammonia synthesis by electrocatalytic nitrate Ammonia (NH3) is one of the most common industrial chemicals. It is not only an indispensable chemical such as fertilizers, pharmaceuticals, dyes, etc., but also considered as an important energy storage medium and carbon- free energy carrier. Currently, industrial-scale production of NH3 relies on the Haber-Bosch process. In this process, NH3 is synthesized by the reaction between H2 and N2 under high pressure and temperature. Meanwhile, the production of H2 is highly energy-intensive and accompanied by the carbon emissions. Therefore, electrocatalytic reaction for NH3 synthesis under ambient pressure and temperature has attracted increasing attention, which is zero carbon emission and powered by cheap renewable electricity. Electrocatalytic nitrate reduction reaction (NIRR) for ammonia synthesis is an appealing alternative to the Haber-Bosch process. Materials and Method Fig. 2 Schematic diagram of preparation of nanoporous Cu alloy catalyst and NITRR
Characterization and properties
Fig. 3 SEM (a) and TEM (b) of nanoporous Cu alloy
Fig. 4 LSV curves of nanoporous Cu and nanoporous Cu alloy in electrolyte with and without NO3-(a); NO2- selectivity (b), NH3 selectivity (c) and Faradaic efficiency (d) of nanoporous Cu and nanoporous Cu alloy Conclusion In this work, three-dimensional nanoporous Cu alloys with interconnected porous network are prepared as a high-performance catalyst for NIRR by a dealloying way. the synergistic combination of nanoporous structure and alloy strategy plays an important role for the NH3 synthesis. Nanoporous Cu alloy exhibits a high NH3 yield rate of 171.43 μmol cm-2 h- 1 at -0.65 V versus RHE under neutral solution which is far more than that of nanoporous Cu.
 | Nanoporous copper alloy for nitrate electroreduction to ammonia Xue Zhou, Zhenduo Cui*, Shengli Zhu* Tianjin University | 

## Slide 2
①建议文本字体-Times New Roman，字体颜色统一黑色； ②海报内容框架默认包含ABSTRACT INTRODUCTION METHODS CONCLUSIONS等； ③多图少字，语句精炼； ④导出图片PNG格式，命名“姓名+学校” ⑤海报整体尽量呈现丰富和多彩，避免图片颜色单一
 | Nanoporous copper alloy for nitrate electroreduction to ammonia Xue Zhou, Zhenduo Cui*, Shengli Zhu* Tianjin University |